Egypt. J. Chem. Vol. 67, No. 12 pp. 129 - 141 (2024)

New Nanoparticle Metal Complexes Based on Cefaclor and 2,2′-Bipyridineligands: Synthesis, Characterization, DFT Studies and Their Antimicrobial Evaluation

H. A. Abdallah, S. A. Sadeek*, M. M. Zareh, M. S. El-Attar, W. A. Zordok, B.Abd El-Wahaab

Department of Chemistry, Faculty of Science, Zagazig University, Zagazig, 44519, Egypt

Supporting Information

FIGURE S1 Infrared spectra for CEF, Bipy and their metal complexes

FIGURE S2 Electronic absorption spectra for CEF, Bipy and their metal complexes

FIGURE S3 Relation of absorbance and molar absorptivity for compounds.

FIGURE S41H NMR spectra for CEF, Bipy,Zn(II) and Cd(II) compounds

FIGURE S5TG,DTGand DTA diagrams for CEFand itsmetal complexes

FIGURE S6 Optimized geometrical structure of complex (1) by using DFT calculations

FIGURE S7Optimized geometrical structure of complex (2) by using DFT calculations

FIGURE S8 Optimized geometrical structure of complex (3) by using DFT calculations

FIGURE S9 Optimized geometry of complex (4) using DFT calculations

FIGURE S10 Optimized geometry of complex (5) using DFT calculations

FIGURE S11 Molecular orbital surfaces and energy levels of CEF, Bipy and their metal complexes

# FIGURE S12 Statistical representation of biological activity for CEF, Bipyand their metal complexes

FIGURE S13 Activity index % for CEF, Bipy and their metalcomplexes

TABLE S11H NMRcalculatedvalues (ppm) for CEF and Bipy

| Compounds | Calculated δ (ppm) |
| --- | --- |
| CEF Bipy |  |

TABLE S2 Equilibrium geometric parameters, bond lengths (Å), bond angles (˚),dihedral angles (˚), total energy(E)and dipole moment(μ) of CEF using DFT calculations

| Bond length (Å) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| C1-C2 C2-C3 C3-N4 N4-C6 C6-S5 C1-S5 C6-C12 C11-C12 N4-C11 C11-O13 C2-Cl7 | 1.522 1.357 1.348 1.445 1.808 1.828 1.589 1.539 1.372 1.204 1.741 |  |  | C3-C8 C8-O9 C8-O10 C12-N14 N14-C15 C15-O17 C15-C18 C18-N20 C18-C23 C23-C24 C23-C28 | 1.369 1.209 1.334 1.446 1.383 1.209 1.524 1.439 1.519 1.348 1.347 |  |  |
| Bond angle (˚) |  |  |  |  |  |  |  |
| C1S5C6 C3N4C6 C3N4C11 N4C3C8 C3C8O10 C3C8C9 O9C8O10 C6N4C11 N4C11O13 C12C11O13 N4C6C12 C11C12N14 |  | 94.10 131.34 128.57 119.09 121.46 123.78 114.76 96.68 133.82 134.37 86.86 111.31 |  | C6C12N14 C12N14C15 N14C15C18 N14C15O17 C18C15O17 C15C18N20 C15C18C23 N20C18C23 C18C23C24 C18C23C28 C1C2Cl7 C3C2Cl7 |  | 127.08 132.08 125.76 116.64 117.57 110.61 115.78 114.66 122.16 120.22 113.62 123.47 |  |
| Dihedral angles (˚) |  |  |  |  |  |  |  |
| O13C11C12N14 C3N7C11O13 N4C3C8O10 N4C3C8O9 O13C11N4C6 C12N14C15O17 |  |  | -62.05 -9.03 2.75 -177.55 -169.75 178.31 | N20C18C23C28 N10C18C23C24 N14C15C18N20 O17C15C18N20 C23C18C15O17 |  |  | 162.91 -18.88 -63.51 114.07 -113.35 |
| E, kcal/mol μ,D |  |  |  | -145698.064 6.434 |  |  |  |

TABLE S3 Equilibrium geometric parameters, bond lengths (Å), bond angles (˚),dihedral angles (˚),  heat of formation (Hf), total energy (E)and dipole moment (μ)of the metal complexes using DFT calculations

| Bond lengths/ Å | Cr(III) | Co(II) | Cu(II) | Zn(II) | Cd(II) |
| --- | --- | --- | --- | --- | --- |
| M-O1 M-O6 M-N13 M-N16 M-N12 M-O17 C5-O6 C9-O10 C2-O1 C11-N12 | 1.972 2.292 1.887 1.889 1.934 1.861 1.196 1.211 1.359 1.529 | 1.958 2.011 1.870 1.871 1.918 1.843 1.198 1.210 1.352 1.525 | 2.118 2.274 2.397 2.392 2.016 2.253 1.196 1.209 1.351 1.523 | 2.198 2.329 2.013 2.015 2.025 2.258 1.197 1.210 1.350 1.522 | 2.339 2.497 2.468 2.465 2.309 2.193 1.198 1209 1.351 1.513 |
| Bond angles/(˚) |  |  |  |  |  |
| O1-M-O6 O1-M-N12 O1-M-N13 O1-M-N16 O1-M-O17 O6-M-N12 O6-M-N13 O6-M-N16 O6-M-O17 N12-M-N13 N12-M-N16 N12-M-O17 N13-M-N16 N13-M-O17 N16-M-O17 | 97.67 169.29 103.88 84.49 77.71 74.99 156.69 95.36 101.71 84.73 103.73 95.94 78.23 91.54 156.74 | 108.51 90.56 91.72 82.23 165.79 74.26 101.23 169.22 84.77 175.42 105.33 88.24 78.93 90.52 84.45 | 109.02 90.90 91.68 82.03 165.53 74.14 101.49 168.93 84.56 175.48 105.59 88.04 78.44 90.41 84.37 | 107.49 91.12 81.79 90.69 166.52 72.78 170.72 103.04 85.09 107.42 175.78 88.01 76.61 85.64 91.11 | 108.01 104.94 86.13 78.92 165.87 67.68 108.99 173.02 85.69 168.92 111.97 83.18 69.96 86.05 87.35 |
| E, kcal/mol Hf, kcal/mol μ, D | -219972.075 -11874.740 13.774 | -233378.349 -12282.772 10.851 | -247316.535 -12339.886 8.794 | -215069.081 -12560.809 11.360 | -214600.515 -12130.185 14.597 |

TABLE S4 Calculated charges on donating sites and energy values (HOMO,  LUMO), Energy gap  ∆E (eV),  hardness (η), global softness (S), electro negativity (χ), absolute softness (σ), chemical potential (Pi), global electrophilicity (ω) and additional electronic charge (∆Nmax) forCEF,Bipyand their metalcomplexes using DFT calculations.

| Parameters | CEF | Bipy | Cr(III) | Co(II) | Cu(II) | Zn(II) | Cd(II) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| M O1 carboxylate O6 lactum O10 amide N12amin N13 bipy N16bipy LUMO, L HOMO, H A = -L I = -H ∆E = L-H η = (I-A)/2 χ = -(H-L/2) σ = 1/ η S = 1/2 η Pi = - χ ω = (Pi)2/2 η ∆Nmax = χ/ η | - -0.365 -0.394 -0.342 -0.352 - - -0.202 -0.324 0.202 0.324 0.122 0.061 0.263 16.393 8.197 -0.263 0.567 4.311 | - - - - - -0.210 -0.212 -0.425 -0.145 0.425 0.145 0.280 0.140 0.285 7.143 3.571 -0.285 0.290 2.036 | 0.381 -0.452 -0.262 -0.310 -0.209 -0.094 -0.065 -0.238 -0.283 0.238 0.283 0.045 0.0225 0.2605 44.444 22.222 -0.2605 1.508 11.578 | -0.063 -0.459 -0.286 -0.349 -0.184 -0.066 -0.038 -0.261 -0.307 0.261 0.307 0.046 0.023 0.284 43.478 21.739 -0.284 1.753 12.348 | 0.160 -0.333 -0.294 -0.351 -0.189 -0.071 -0.057 -0.239 -0.312 0.239 0.312 0.073 0.0365 0.1755 27.397 13.698 -0.1755 0.4219 4.808 | 0.098 -0.488 -0.306 -0.349 -0.203 -0.089 -0.069 -0.241 -0.331 0.241 0.331 0.090 0.045 0.286 22.222 11.111 -0.286 0.9088 6.356 | 0.329 -0.484 -0.332 -0.348 -0.242 -0.134 -0.117 -0.239 -0.336 0.239 0.336 0.0485 0.0243 0.2875 41.152 20.576 -0.2875 1.7007 11.8313 |

(I) is an ionization energy               (A) is an electron affinity

TABLE S5: Composition of Frontier molecular orbital formetal complexesusing DFT/B3LYP/Cep-31G.

|  | (1) |  |  | (2) |  |
| --- | --- | --- | --- | --- | --- |
|  | H | L |  | H | L |
| Cr | 8.4% | 66.4% | Co | 12.8% | 74.4% |
| CEF | 0.0% | 16.6% | CEF | 87.2% | 13.7% |
| Bipy | 83.7% | 4.3% | Bipy | 0.0% | 8.3% |
| H2O | 7.9% | 12.7% | H2O | 0.0% | 3.6% |
|  | (3) |  |  | (4) |  |
|  | H | L |  | H | L |
| Cu | 37.6% | 39.9% | Zn | 29.4% | 0.0% |
| CEF | 24.3% | 29.8% | CEF | 70.6% | 0.0% |
| Bipy | 18.8% | 12.9% | Bipy | 0.0% | 100% |
| H2O | 19.3% | 17.4% | H2O | 0.0% | 0.0% |
|  | (5) |  |  |  |  |
|  | H | L |  |  |  |
| Cd | 0.0% | 0.0% |  |  |  |
| CEF | 100% | 0.0% |  |  |  |
| Bipy | 0.0% | 98.6% |  |  |  |
| H2O | 0.0% | 1.4% |  |  |  |